File MH48828	Page T1-1 of 19	Issued:  2012-03-26

TEST RECORD NO. 1

The manufacturer submitted samples to perform testing per the requirements in NFPA 2112, Standard on Flame Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition.  The results were in compliance with the requirements.

Results relate only to the items tested.

SAMPLES

Standard coveralls and yardage of the following fabrics:

Style Designation	Weight (oz/yd²)	Material Composition	Knit	Finish	
	Unfinished	Finished				
2018FW	7.0	7.75	100% Cotton	Jersey	Frame FR	
1580FR	11.2	12.0	100% Cotton	Single Sided Fleece Knit	Frame FR	
1852FM	6.5	7.25	100% Cotton	Interlock	Frame FR	
8581FR	7.4	7.9	73% Supima Cotton/24% Modal Cellulose/3% Spandex	Plaited	Frame FR	

TESTS CONDUCTED

Flame Resistance Test
Heat and Thermal Shrinkage Resistance Test
Thermal Protective Performance Test
Manikin Test

File MH48828	Page T1-2 of 19	Issued:  2012-03-26

FLAME RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.3	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Flame Resistance Test	8.3	03-LO-W0079	

2.0	RESULTS - FABRICS
(A)
Article:	Outer Shell Fabric	
Description:	Style 2018FW, 100% Cotton, Jersey Knit with Frame FR Finish	
Color:	Light Green	
Weight:	7.75 (7.0 Unfinished)	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Conditioning	Specimen	Warp (Wales)	Fill (Courses)	
		Afterflame (s)	Char Length (mm)	Melt/ Drip [Y/N]	Afterflame (s)	Char Length (mm)	Melt/ Drip [Y/N]	
As Received	1	0.96	73	N/N	0.92	76	N/N	
	2	1.13	76	N/N	0.84	77	N/N	
	3	0.86	74	N/N	0.83	68	N/N	
	4	0.76	78	N/N	0.80	76	N/N	
	5	0.66	67	N/N	0.85	70	N/N	
	Average	0.87	74	N/A	0.85	73	N/A	
	Rounded Average	0.8	75	N/A	0.8	72	N/A	
After Laundering	1	0.87	73	N/N	0.73	75	N/N	
	2	0.84	71	N/N	0.87	72	N/N	
	3	0.76	84	N/N	1.00	72	N/N	
	4	0.63	65	N/N	0.98	74	N/N	
	5	0.68	71	N/N	0.78	66	N/N	
	Average	0.76	73	N/A	0.87	72	N/A	
	Rounded Average	0.8	72	N/A	0.8	72	N/A	

File MH48828	Page T1-3 of 19	Issued:  2012-03-26

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT'D)	NFPA 2112-2012, Section 8.3	

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T1-4 of 19	Issued:  2012-03-26

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT'D)	NFPA 2112-2012, Section 8.3	

2.0	RESULTS - FABRICS
(B)
Article:	Outer Shell Fabric	
Description:	Style 1580FR, 100% Cotton, Single Sided Fleece Knit with Frame FR Finish	
Color:	Navy	
Weight:	12.0 (11.2 Unfinished)	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Conditioning	Specimen	Warp (Wales)	Fill (Courses)	
		Afterflame (s)	Char Length (mm)	Melt/ Drip [Y/N]	Afterflame (s)	Char Length (mm)	Melt/ Drip [Y/N]	
As Received	1	0.0	34.0	N	0.0	62.0	N	
	2	0.0	39.0	N	0.0	41.0	N	
	3	0.0	20.0	N	0.0	50.0	N	
	4	0.0	31.0	N	0.0	57.0	N	
	5	0.0	26.0	N	0.0	56.0	N	
	Average	0.0	30.0	N/A	0.0	53.2	N/A	
	Rounded Average	0.0	30	N/A	0.0	54	N/A	
After Laundering	1	0.0	33.0	N	0.0	30.0	N	
	2	0.0	31.0	N	0.0	39.0	N	
	3	0.0	33.0	N	0.0	36.0	N	
	4	0.0	32.0	N	0.0	21.0	N	
	5	0.0	37.0	N	0.0	28.0	N	
	Average	0.0	33.2	N/A	0.0	30.8	N/A	
	Rounded Average	0.0	33	N/A	0.0	30	N/A	

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T1-5 of 19	Issued:  2012-03-26

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT'D)	NFPA 2112-2012, Section 8.3	

2.0	RESULTS - FABRICS
(C)
Article:	Outer Shell Fabric	
Description:	Style 1852FM, 100% Cotton, Interlock Knit with Frame FR Finish	
Color:	Tan	
Weight:	7.25 (6.5 Unfinished)	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Conditioning	Specimen	Warp (Wales)	Fill (Courses)	
		Afterflame (s)	Char Length (mm)	Melt/ Drip [Y/N]	Afterflame (s)	Char Length (mm)	Melt/ Drip [Y/N]	
As Received	1	0.0	22.0	N	0.0	47.0	N	
	2	0.0	77.0	N	0.0	66.0	N	
	3	0.0	56.0	N	0.0	36.0	N	
	4	0.0	67.0	N	0.0	41.0	N	
	5	0.0	72.0	N	0.0	54.0	N	
	Average	0.0	58.8	N/A	0.0	48.8	N/A	
	Rounded Average	0.0	60	N/A	0.0	48	N/A	
After Laundering	1	0.0	56.0	N	0.0	86.0	N	
	2	0.0	85.0	N	0.0	79.0	N	
	3	0.0	68.0	N	0.0	69.0	N	
	4	0.0	61.0	N	0.0	75.0	N	
	5	0.0	71.0	N	0.0	78.0	N	
	Average	0.0	68.2	N/A	0.0	77.4	N/A	
	Rounded Average	0.0	69	N/A	0.0	78	N/A	

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T1-6 of 19	Issued:  2012-03-26

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT'D)	NFPA 2112-2012, Section 8.3	

2.0	RESULTS - FABRICS
(D)
Article:	Outer Shell Fabric	
Description:	Style 8581FR, 73% Supima Cotton/24% Modal Cellulose/3% Spandex, Plaited Knit with Frame FR Finish	
Color:	Navy	
Weight:	7.9 (7.4 Unfinished)	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Conditioning	Specimen	Warp (Wales)	Fill (Courses)	
		Afterflame (s)	Char Length (mm)	Melt/ Drip [Y/N]	Afterflame (s)	Char Length (mm)	Melt/ Drip [Y/N]	
As Received	1	0.0	83.0	N	0.0	71.0	N	
	2	0.0	84.0	N	0.0	73.0	N	
	3	0.0	80.0	N	0.0	63.0	N	
	4	0.0	91.0	N	0.0	68.0	N	
	5	0.0	76.0	N	0.0	74.0	N	
	Average	0.0	82.8	N/A	0.0	69.8	N/A	
	Rounded Average	0.0	84	N/A	0.0	69	N/A	
After Laundering	1	0.0	77.0	N	0.0	70.0	N	
	2	0.0	89.0	N	0.0	65.0	N	
	3	0.0	82.0	N	0.0	65.0	N	
	4	0.0	86.0	N	0.0	70.0	N	
	5	0.0	73.0	N	0.0	69.0	N	
	Average	0.0	81.4	N/A	0.0	67.8	N/A	
	Rounded Average	0.0	81	N/A	0.0	69	N/A	

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T1-7 of 19	Issued:  2012-03-26

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.4	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat and Thermal Shrinkage Resistance Test	8.4	03-LO-W0035	

2.0	RESULTS - FABRICS
(A)
Article:	Outer Shell Fabric	
Description:	Style 2018FW, 100% Cotton, Jersey Knit with Frame FR Finish	
Color:	Light Green	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

As Received	
Specimen	Warp Percent Shrinkage	Fill Percent Shrinkage	Melt [Y/N]	Drip [Y/N]	Separate [Y/N]	Ignite [Y/N]	
	1	2	3	1	2	3					
1	-0.5	-0.5	-0.5	0.0	0.0	0.0	N	N	N	N	
2	-0.5	-0.5	-0.5	0.0	0.0	0.0	N	N	N	N	
3	-0.5	-0.5	-0.5	0.0	0.0	0.0	N	N	N	N	
Average	-0.5	0.0	N/A	
After Laundering	
Specimen	Warp Percent Shrinkage	Fill Percent Shrinkage	Melt [Y/N]	Drip [Y/N]	Separate [Y/N]	Ignite [Y/N]	
	1	2	3	1	2	3					
1	-1.0	-1.0	-1.0	-0.5	-0.5	-0.5	N	N	N	N	
2	-1.0	-1.0	-0.5	-0.5	-0.5	-0.5	N	N	N	N	
3	-0.5	-0.5	-1.0	-0.5	-0.5	-0.5	N	N	N	N	
Average	-0.8	-0.5	N/A	

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T1-8 of 19	Issued:  2012-03-26

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.4	

2.0	RESULTS - FABRICS
(B)
Article:	Outer Shell Fabric	
Description:	Style 1580FR, 100% Cotton, Single Sided Fleece Knit with Frame FR Finish	
Color:	Navy	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

As Received	
Specimen	Warp Percent Shrinkage	Fill Percent Shrinkage	Melt [Y/N]	Drip [Y/N]	Separate [Y/N]	Ignite [Y/N]	
	1	2	3	1	2	3					
1	+0.5	+0.5	+0.5	-1.0	-1.0	-0.5	N	N	N	N	
2	+1.0	+1.0	+1.0	-1.0	-1.0	-1.0	N	N	N	N	
3	+0.5	+0.5	+0.5	-1.0	-1.0	-1.0	N	N	N	N	
Average	+0.7	-0.9	N/A	
After Laundering	
Specimen	Warp Percent Shrinkage	Fill Percent Shrinkage	Melt [Y/N]	Drip [Y/N]	Separate [Y/N]	Ignite [Y/N]	
	1	2	3	1	2	3					
1	-0.5	-0.5	-0.5	-0.5	-0.5	-0.5	N	N	N	N	
2	-0.5	-0.5	-0.5	-0.5	-0.5	-0.5	N	N	N	N	
3	-0.5	-0.5	-0.5	-0.5	-0.5	-0.5	N	N	N	N	
Average	-0.5	-0.5	N/A	

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T1-9 of 19	Issued:  2012-03-26

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.4	

2.0	RESULTS - FABRICS
(C)
Article:	Outer Shell Fabric	
Description:	Style 1852FM, 100% Cotton, Interlock Knit with Frame FR Finish	
Color:	Tan	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

As Received	
Specimen	Warp Percent Shrinkage	Fill Percent Shrinkage	Melt [Y/N]	Drip [Y/N]	Separate [Y/N]	Ignite [Y/N]	
	1	2	3	1	2	3					
1	+1.0	+1.0	+1.0	-1.0	-1.0	-1.0	N	N	N	N	
2	+1.5	+1.0	+1.0	-1.0	-1.5	-1.0	N	N	N	N	
3	+1.5	+1.5	+1.5	-1.5	-2.0	-1.5	N	N	N	N	
Average	+1.2	-1.3	N/A	
After Laundering	
Specimen	Warp Percent Shrinkage	Fill Percent Shrinkage	Melt [Y/N]	Drip [Y/N]	Separate [Y/N]	Ignite [Y/N]	
	1	2	3	1	2	3					
1	0.0	0.0	-0.5	-0.5	-0.5	-0.5	N	N	N	N	
2	-0.5	0.0	-0.5	-0.5	-0.5	-0.5	N	N	N	N	
3	-0.5	-0.5	-0.5	-1.5	-1.5	-1.5	N	N	N	N	
Average	-0.3	-0.8	N/A	

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T1-10 of 19	Issued:  2012-03-26

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.4	

2.0	RESULTS - FABRICS
(D)
Article:	Outer Shell Fabric	
Description:	Style 8581FR, 73% Supima Cotton/24% Modal Cellulose/3% Spandex, Plaited Knit with Frame FR Finish	
Color:	Navy	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

As Received	
Specimen	Warp Percent Shrinkage	Fill Percent Shrinkage	Melt [Y/N]	Drip [Y/N]	Separate [Y/N]	Ignite [Y/N]	
	1	2	3	1	2	3					
1	+5.5	+5.5	+5.0	+1.0	+0.5	+1.0	N	N	N	N	
2	+5.0	+5.0	+5.0	+1.0	+1.0	+1.0	N	N	N	N	
3	+5.5	+5.0	+5.5	+0.5	+1.0	+0.5	N	N	N	N	
Average	+5.2	+0.8	N/A	
After Laundering	
Specimen	Warp Percent Shrinkage	Fill Percent Shrinkage	Melt [Y/N]	Drip [Y/N]	Separate [Y/N]	Ignite [Y/N]	
	1	2	3	1	2	3					
1	+6.0	+6.0	+6.0	-1.0	-1.0	-1.0	N	N	N	N	
2	+6.0	+5.5	+5.5	-0.5	-0.5	-0.5	N	N	N	N	
3	+5.0	+6.0	+5.0	-0.5	-0.5	-0.5	N	N	N	N	
Average	+5.7	-0.7	N/A	

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T1-11 of 19	Issued:  2012-03-26

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.2	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat Transfer Performance (HTP) Test	8.2	03-LO-W0041	

2.0	RESULTS 
(A)
Article:	Outer Shell Fabric	
Description:	Style 2018FW, 100% Cotton, Jersey Knit with Frame FR Finish	
Color:	Light Green	

CONDITIONING: SEE TABLE BELOW

Specimen	Contact Test HTP Rating (cal/cm2)	Spaced Test HTP Rating
(cal/cm2)	
	As Received	After 3 Launderings	As Received	After 3 Launderings	
1	9.6	9.8	10.4	10.6	
2	9.9	9.7	9.9	10.7	
3	9.5	10.2	9.9	10.5	
Average	9.7	9.9	10.1	10.6	
Individuals within 10% of Average [Y/N]	Y	Y	Y	Y	

3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than
25 J/cm2 (6.0 cal/cm2).
2. The average contact HTP rating shall not be less than
12.6 J/cm2 (3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T1-12 of 19	Issued:  2012-03-26

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS (CONT’D)	NFPA 2112-2012, Section 8.2	

2.0	RESULTS 
(B)
Article:	Outer Shell Fabric	
Description:	Style 1580FR, 100% Cotton, Single Sided Fleece Knit with Frame FR Finish	
Color:	Navy	

CONDITIONING: SEE TABLE BELOW

Specimen	Contact Test HTP Rating (cal/cm2)	Spaced Test HTP Rating
(cal/cm2)	
	As Received	After 3 Launderings	As Received	After 3 Launderings	
1	16.4	20.2	19.6	21.5	
2	17.6	20.1	19.4	21.8	
3	16.5	19.5	16.9	22.1	
Average	16.8	19.9	18.6	21.8	
Individuals within 10% of Average [Y/N]	Y	Y	Y	Y	

3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than
25 J/cm2 (6.0 cal/cm2).
2. The average contact HTP rating shall not be less than
12.6 J/cm2 (3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T1-13 of 19	Issued:  2012-03-26

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS (CONT’D)	NFPA 2112-2012, Section 8.2	

2.0	RESULTS 
(C)
Article:	Outer Shell Fabric	
Description:	Style 1852FM, 100% Cotton, Interlock Knit with Frame FR Finish	
Color:	Tan	

CONDITIONING: SEE TABLE BELOW

Specimen	Contact Test HTP Rating (cal/cm2)	Spaced Test HTP Rating
(cal/cm2)	
	As Received	After 3 Launderings	As Received	After 3 Launderings	
1	9.4	10.3	9.8	10.7	
2	9.5	10.5	9.8	10.7	
3	9.3	10.1	9.7	10.7	
Average	9.4	10.3	9.8	10.7	
Individuals within 10% of Average [Y/N]	Y	Y	Y	Y	

3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than
25 J/cm2 (6.0 cal/cm2).
2. The average contact HTP rating shall not be less than
12.6 J/cm2 (3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T1-14 of 19	Issued:  2012-03-26

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS (CONT’D)	NFPA 2112-2012, Section 8.2	

2.0	RESULTS 
(D)
Article:	Outer Shell Fabric	
Description:	Style 8581FR, 73% Supima Cotton/24% Modal Cellulose/3% Spandex, Plaited Knit with Frame FR Finish	
Color:	Navy	

CONDITIONING: SEE TABLE BELOW

Specimen	Contact Test HTP Rating (cal/cm2)	Spaced Test HTP Rating
(cal/cm2)	
	As Received	After 3 Launderings	As Received	After 3 Launderings	
1	12.1	11.7	12.7	12.8	
2	11.5	12.1	12.8	12.9	
3	11.9	11.8	13.2	12.8	
Average	11.8	11.9	12.9	12.8	
Individuals within 10% of Average [Y/N]	Y	Y	Y	Y	

3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than
25 J/cm2 (6.0 cal/cm2).
2. The average contact HTP rating shall not be less than
12.6 J/cm2 (3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T1-15 of 19	Issued:  2012-03-26

MANIKIN TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.5	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Manikin Test	8.5	03-LO-W0043	

2.0	RESULTS
(1)
Article:	Outer Shell Fabric	
Description:	Style 8581FR, 73% Supima Cotton/24% Modal Cellulose/3% Spandex, Plaited Knit with Frame FR Finish	
Color:	Navy	
Weight:	7.9 (7.4 Unfinished)	oz./yd²	
Test Report ID:	120307G, 120307N, 120307Q		

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	10.66	
2	9.84	
3	11.48	
Average	10.66	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T1-16 of 19	Issued:  2012-03-26

MANIKIN TEST – GARMENT FABRICS (CONT’D)	NFPA 2112-2012, Section 8.5	

2.0	RESULTS
(2)
Article:	Outer Shell Fabric	
Description:	Style 1580FR, 100% Cotton, Single Sided Fleece Knit with Frame FR Finish	
Color:	Navy	
Weight:	12 (11.2 Unfinished)	oz./yd²	
Test Report ID:	120307H, 120307K, 120307R	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	7.38	
2	7.38	
3	8.20	
Average	7.65	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T1-17 of 19	Issued:  2012-03-26

MANIKIN TEST – GARMENT FABRICS (CONT’D)	NFPA 2112-2012, Section 8.5	

2.0	RESULTS
(3)
Article:	Outer Shell Fabric	
Description:	Style 1852FM, 100% Cotton, Interlock Knit with Frame FR Finish	
Color:	Tan	
Weight:	7.25 (6.5 Unfinished)	oz./yd²	
Test Report ID:	120307I, 120307L, 120307O	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	16.39	
2	17.21	
3	15.57	
Average	16.39	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T1-18 of 19	Issued:  2012-03-26

MANIKIN TEST – GARMENT FABRICS (CONT’D)	NFPA 2112-2012, Section 8.5	

2.0	RESULTS
(4)
Article:	Outer Shell Fabric	
Description:	Style 2018FW, 100% Cotton, Jersey Knit with Frame FR Finish	
Color:	Light Green	
Weight:	7.75 (7.0 Unfinished)	oz./yd²	
Test Report ID:	120307J, 120307M, 120307P	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	12.30	
2	13.11	
3	13.11	
Average	12.84	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T1-19 of 19	Issued:  2012-03-26

Test Record No. 1 Summary

The results of this investigation, including construction review and testing, indicate that the products evaluated comply with the applicable requirements in NFPA 2112, Standard on Flame-Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition and, therefore, such products are judged eligible to bear UL's Mark as described on the Conclusion Page of this Report. Any information and documentation involving UL Mark services are provided on behalf of UL LLC (UL) or any authorized licensee of UL.

File MH48828	Page T2-1 of 19	Issued:  2012-03-26
	New:  2013-05-20

TEST RECORD NO. 1

The manufacturer submitted samples to perform testing per the requirements in NFPA 2112, Standard on Flame Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition.  The results were in compliance with the requirements.

Results relate only to the items tested.

SAMPLES

Standard coveralls and yardage of the following fabrics:

Style Designation	Weight (oz/yd²)	Material Composition	Knit	Finish	
	Unfinished	Finished				
3108FW	6.8	8.0	100% Cotton	Textured Double Knit	FR	
865HFR	11.2	12.5	95% Cotton/5% Spandex	Single Sided Fleece Knit	FR	
1582FW	5.8	7.0	100% Cotton	Double Pique Knit	FR	
545CFM	5.0	6.0	100% Cotton	Single Jersey Knit	FR	

TESTS CONDUCTED

Flame Resistance Test
Heat and Thermal Shrinkage Resistance Test
Thermal Protective Performance Test
Manikin Test

NOTE

Per the manufacturer’s request, the finish of existing styles 2018FW, 1580FR, 1852FM, 8581FR was changed to “FR” for consistency purposes.  The fabrics remain unchanged from the original evaluation.

File MH48828	Page T2-2 of 19	Issued:  2012-03-26
	New:  2013-05-20

FLAME RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.3	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Flame Resistance Test	8.3	03-LO-W0079	

2.0	RESULTS – FABRICS
(A)
Article:	Outer Shell	
Description:	Style 3108FW, 100% Cotton with FR Finish	
Color:	Grey	
Weight:	8.0 (6.8 Unfinished)	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Software Validation: 76083

File MH48828	Page T2-3 of 19	Issued:  2012-03-26
	New:  2013-05-20

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT'D)	NFPA 2112-2012, Section 8.3	

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T2-4 of 19	Issued:  2012-03-26
	New:  2013-05-20

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.3	

2.0	RESULTS – FABRICS
(B)
Article:	Outer Shell	
Description:	Style 865HFR, 95% Cotton/5% Spandex with FR Finish	
Color:	Navy	
Weight:	12.5 (11.2 Unfinished)	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T2-5 of 19	Issued:  2012-03-26
	New:  2013-05-20

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.3	

2.0	RESULTS – FABRICS
(C)
Article:	Outer Shell	
Description:	Style 1582FW, 100% Cotton with FR Finish	
Color:	Grey	
Weight:	7.0 (5.8 Unfinished)	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T2-6 of 19	Issued:  2012-03-26
	New:  2013-05-20

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.3	

2.0	RESULTS – FABRICS
(D)
Article:	Outer Shell	
Description:	Style 545CFM, 100% Cotton with FR Finish	
Color:	Grey	
Weight:	6.0 (5.0 Unfinished)	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T2-7 of 19	Issued:  2012-03-26
	New:  2013-05-20

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.4	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat and Thermal Shrinkage Resistance Test	8.4	03-LO-W0035	

2.0	RESULTS - FABRICS
(A)
Article:	Outer Shell	
Description:	Style 3108FW, 100% Cotton with FR Finish	
Color:	Grey	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T2-8 of 19	Issued:  2012-03-26
	New:  2013-05-20

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.4	

2.0	RESULTS - FABRICS
(B)
Article:	Outer Shell	
Description:	Style 865HFR, 95% Cotton/5% Spandex with FR Finish	
Color:	Navy	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T2-9 of 19	Issued:  2012-03-26
	New:  2013-05-20

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.4	

2.0	RESULTS - FABRICS
(C)
Article:	Outer Shell	
Description:	Style 1582FW, 100% Cotton with FR Finish	
Color:	Grey	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T2-10 of 19	Issued:  2012-03-26
	New:  2013-05-20

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.4	

2.0	RESULTS - FABRICS
(D)
Article:	Outer Shell	
Description:	Style 545CFM, 100% Cotton with FR Finish	
Color:	Grey	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T2-11 of 19	Issued:  2012-03-26
	New:  2013-05-20

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.2	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat Transfer Performance (HTP) Test	8.2	03-LO-W0041	

2.0	RESULTS
(A)
Article:	Outer Shell	
Description:	Style 3108FW, 100% Cotton with FR Finish	
Color:	Grey	

CONDITIONING: SEE TABLE BELOW
 Software Validation: 76083
3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than 25 J/cm2 (6.0 cal/cm2).
2. The average contact HTP rating shall not be less than 12.6 J/cm2 (3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T2-12 of 19	Issued:  2012-03-26
	New:  2013-05-20

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.2	

2.0	RESULTS
(B)
Article:	Outer Shell	
Description:	Style 865HFR, 95% Cotton/5% Spandex with FR Finish	
Color:	Navy	

CONDITIONING: SEE TABLE BELOW
 Software Validation: 76083
3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than 25 J/cm2 (6.0 cal/cm2).
2. The average contact HTP rating shall not be less than 12.6 J/cm2 (3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T2-13 of 19	Issued:  2012-03-26
	New:  2013-05-20

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.2	

2.0	RESULTS
(C)
Article:	Outer Shell	
Description:	Style 1582FW, 100% Cotton with FR Finish	
Color:	Grey	

CONDITIONING: SEE TABLE BELOW
 Software Validation: 76083
3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than 25 J/cm2 (6.0 cal/cm2).
2. The average contact HTP rating shall not be less than 12.6 J/cm2 (3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T2-14 of 19	Issued:  2012-03-26
	New:  2013-05-20

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.2	

2.0	RESULTS
(D)
Article:	Outer Shell	
Description:	Style 545CFM, 100% Cotton with FR Finish	
Color:	Grey	

CONDITIONING: SEE TABLE BELOW
 Software Validation: 76083
3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than 25 J/cm2 (6.0 cal/cm2).
2. The average contact HTP rating shall not be less than 12.6 J/cm2 (3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T2-15 of 19	Issued:  2012-03-26
	New:  2013-05-20

MANIKIN TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.5	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Manikin Test	8.5	03-LO-W0043	

2.0	RESULTS
(A)
Article:	Outer Shell	
Description:	Style 3108FW, 100% Cotton with FR Finish, 8.0 OSY	
Color:	Grey	
Test Report ID:	130516H, 130516I, 130516J	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	8.20	
2	8.20	
3	7.38	
Average	7.93	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T2-16 of 19	Issued:  2012-03-26
	New:  2013-05-20

MANIKIN TEST – GARMENT FABRICS (CONT’D)	NFPA 2112-2012, Section 8.5	

2.0	RESULTS
(B)
Article:	Outer Shell	
Description:	Style 865HFR, 95% Cotton/5% Spandex with FR Finish, 12.5 OSY	
Color:	Navy	
Test Report ID:	130516K, 130516L, 130516M	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	6.56	
2	6.56	
3	6.56	
Average	6.56	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T2-17 of 19	Issued:  2012-03-26
	New:  2013-05-20

MANIKIN TEST – GARMENT FABRICS (CONT’D)	NFPA 2112-2012, Section 8.5	

2.0	RESULTS
(C)
Article:	Outer Shell	
Description:	Style 1582FW, 100% Cotton with FR Finish, 7.0 OSY	
Color:	Grey	
Test Report ID:	130516E, 130516F, 130516G	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	17.21	
2	19.67	
3	17.21	
Average	18.03	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T2-18 of 19	Issued:  2012-03-26
	New:  2013-05-20

MANIKIN TEST – GARMENT FABRICS (CONT’D)	NFPA 2112-2012, Section 8.5	

2.0	RESULTS
(D)
Article:	Outer Shell	
Description:	Style 545CFM, 100% Cotton with FR Finish, 6.0 OSY	
Color:	Grey	
Test Report ID:	130516B, 130516C, 130516D	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	26.23	
2	27.05	
3	22.13	
Average	25.14	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T2-19 of 19	Issued:  2012-03-26
	New:  2013-05-20

Test Record No. 2 Summary

The results of this investigation, including construction review and testing, indicate that the products evaluated comply with the applicable requirements in NFPA 2112, Standard on Flame-Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition and, therefore, such products are judged eligible to bear UL's Mark as described on the Conclusion Page of this Report. Any information and documentation involving UL Mark services are provided on behalf of UL LLC (UL) or any authorized licensee of UL.

Test Record No. 2 By:	Reviewed By:	
		
Andrew Kaiser	Gregg A. Skelly	
Project Engineer	Staff Engineering Associate	
Conformity Assessment Services	Conformity Assessment Services	

File MH48828	Page T3-1 of 4	Issued:  2012-03-26
	New:  2013-07-25

TEST RECORD NO. 3

The manufacturer submitted samples to perform testing per the requirements in NFPA 2112, Standard on Flame-Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition (2013-03-07).  The results were in compliance with the requirements.

Test results relate only to the items tested.

SAMPLES

Yardage of the following styles:

Style Designation	Weight (oz/yd²)	Material Composition	Weave	Finish	
	Unfinished	Finished				
168LFR	6.9	7.5	95% Cotton/5% Spandex	Rib Knit	FR	
2176FR	14.5	15.5	98% Cotton/2% Spandex	Rib Knit	FR	

TESTS CONDUCTED

Heat and Thermal Shrinkage Resistance

NOTES

No additional testing was determined to be necessary since these materials are considered “other textile materials”.

File MH48828	Page T3-2 of 4	Issued:  2012-03-26
	New:  2013-07-25

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.4	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat and Thermal Shrinkage Resistance Test	8.4	03-LO-W0035	

2.0	RESULTS - REFLECTIVE STRIPING AND OTHER GARMENT MATERIALS

Article:	Trim (Collar, Cuff) Fabric	
Description:	Style 168LFR, 95% Cotton/5% Spandex, Rib Knit with FR Finish	
Color:	Tan	

CONDITIONING: AS RECEIVED

Specimen	Melt
[Y/N]	Drip
[Y/N]	Separate
[Y/N]	Ignite
[Y/N]	
1	N	N	N	N	
2	N	N	N	N	
3	N	N	N	N	

3.0	COMPLIANCE CRITERIA - REFLECTIVE STRIPING AND OTHER GARMENT MATERIALS

3.1	Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T3-3 of 4	Issued:  2012-03-26
	New:  2013-07-25

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS (CONT'D)	NFPA 2112-2012, Section 8.4	

2.0	RESULTS - REFLECTIVE STRIPING AND OTHER GARMENT MATERIALS

Article:	Trim (Collar, Cuff) Fabric	
Description:	Style 2176FR, 98% Cotton/2% Spandex, Rib Knit with FR Finish	
Color:	Grey	

CONDITIONING: AS RECEIVED

Specimen	Melt
[Y/N]	Drip
[Y/N]	Separate
[Y/N]	Ignite
[Y/N]	
1	N	N	N	N	
2	N	N	N	N	
3	N	N	N	N	

3.0	COMPLIANCE CRITERIA - REFLECTIVE STRIPING AND OTHER GARMENT MATERIALS

3.1	Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T3-4 of 4	Issued:  2012-03-26
	New:  2013-07-25

Test Record No. 3 Summary

The results of this investigation, including construction review and testing, indicate that the products evaluated comply with the applicable requirements in NFPA 2112, Standard on Flame-Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition (2013-03-07) and, therefore, such products are judged eligible to bear UL's Mark as described on the Conclusion Page of this Report. Any information and documentation involving UL Mark services are provided on behalf of UL LLC (UL) or any authorized licensee of UL.

Test Record No. 3 By:	Reviewed By:	
		
Andrew Kaiser	Amanda H. Newsom	
Project Engineer	Senior Project Engineer	
Conformity Assessment Services	Conformity Assessment Services	

File MH48828	Page T4-1 of 7	Issued:  2012-03-26
	New:  2014-06-04

TEST RECORD NO. 4

The manufacturer submitted samples to perform testing per the requirements in NFPA 2112, Standard on Flame Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition (2013-08-01).  The results were in compliance with the requirements.

Results relate only to the items tested.

SAMPLES

Standard coveralls and yardage of the following fabrics:

Style Designation	Weight (oz/yd²)	Material Composition	Weave	Finish	
	Unfinished	Finished				
5601FP	6.5	7.2	100% Cotton	Twill	FR	

TESTS CONDUCTED

Flame Resistance Test
Heat and Thermal Shrinkage Resistance Test
Thermal Protective Performance Test
Manikin Test

No additional testing was determined to be necessary.

File MH48828	Page T4-2 of 7	Issued:  2012-03-26
	New:  2014-06-04

FLAME RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.3	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Flame Resistance Test	8.3	03-LO-W0079	

2.0	RESULTS – FABRICS AND COLD WEATHER INSULATION MATERIALS

Article:	Outer Shell Fabric	
Description:	Style 5601FP, 100% Cotton, Twill Weave with Frame FR Finish	
Color:	White with Blue and Red Stripes	
Unfinished Weight:	6.5	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Software Validation: 76083

File MH48828	Page T4-3 of 7	Issued:  2012-03-26
	New:  2014-06-04

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT'D)	NFPA 2112-2012, Section 8.3	

3.0	COMPLIANCE CRITERIA – FABRICS AND COLD WEATHER INSULATION MATERIALS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T4-4 of 7	Issued:  2012-03-26
	New:  2014-06-04

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.4	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat and Thermal Shrinkage Resistance Test	8.4	03-LO-W0035	

2.0	RESULTS - FABRICS

Article:	Outer Shell Fabric	
Description:	Style 5601FP, 100% Cotton, Twill Weave with Frame FR Finish	
Color:	White with Blue and Red Stripes	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T4-5 of 7	Issued:  2012-03-26
	New:  2014-06-04

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.2	

1.0	PROCEDURE

1.1	Test in accordance with:
TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat Transfer Performance (HTP) Test	8.2	03-LO-W0041	

2.0	RESULTS
Article:	Outer Shell Fabric	
Description:	Style 5601FP, 100% Cotton, Twill Weave with Frame FR Finish	
Color:	White with Blue and Red Stripes	

CONDITIONING: SEE TABLE BELOW

Software Validation: 76083

3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than 25 J/cm2 
	(6.0 cal/cm2).
2. The average contact HTP rating shall not be less than 12.6 J/cm2 
(3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T4-6 of 7	Issued:  2012-03-26
	New:  2014-06-04

MANIKIN TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.5	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Manikin Test	8.5	03-LO-W0043	

2.0	RESULTS

Article:	Outer Shell Fabric	
Description:	Style 5601FP, 100% Cotton, Twill Weave with Frame FR Finish	
Color:	White with Blue and Black Stripes	
Test Report ID:	140501O, 140501P, 140501Q	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	18.85	
2	19.67	
3	22.95	
Average	20.49	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T4-7 of 7	Issued:  2012-03-26
	New:  2014-06-04

Test Record No. 4 Summary

The results of this investigation, including construction review and testing, indicate that the products evaluated comply with the applicable requirements in NFPA 2112, Standard on Flame-Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition (2013-08-01) and, therefore, such products are judged eligible to bear UL's Mark as described on the Conclusion Page of this Report. Any information and documentation involving UL Mark services are provided on behalf of UL LLC (UL) or any authorized licensee of UL.

Test Record No. 4 By:	Reviewed By:	
Andrew Kaiser	Gregg A. Skelly	
Senior Project Engineer	Staff Engineering Associate	
Conformity Assessment Services	Conformity Assessment Services	

File MH48828	Page T5-1 of 1	Issued:  2012-03-26
	New:  2014-10-28

TEST RECORD NO. 5

No testing was determined to be necessary to remove the following fabric from this report since it is being added to a new section 3 (adding complimentary recognition to CAN/CGSB 155.20) of this report.

Style Designation	Weight (oz/yd²)	Material Composition	Knit	Finish	
	Unfinished	Finished				
2018FW	7.0	7.75	100% Cotton	Jersey	Frame FR	

Test Record No. 5 Summary

The results of this investigation, including construction review and testing, indicate that the products evaluated comply with the applicable requirements in NFPA 2112, Standard on Flame-Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition (2013-08-01) and, therefore, such products are judged eligible to bear UL's Mark as described on the Conclusion Page of this Report. Any information and documentation involving UL Mark services are provided on behalf of UL LLC (UL) or any authorized licensee of UL.

Test Record No. 5 By:	Reviewed By:	
		
Amanda H. Newsom	Gregg A. Skelly	
Senior Project Engineer	Staff Engineering Associate	
Conformity Assessment Services	Conformity Assessment Services	

File MH48828	Page T6-1 of 8	Issued:  2012-03-26
	New:  2015-02-06

TEST RECORD NO. 6

The manufacturer submitted samples to perform testing per the requirements in NFPA 2112, Standard on Flame Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition (2013-08-01).  The results were in compliance with the requirements.

Results relate only to the items tested.

SAMPLES

Standard coveralls and yardage of the following fabric:

Style Designation	Weight (oz/yd²)	Material Composition	Weave	Finish	
	Unfinished	Finished				
8812FR	6.0	7.1	88% Cotton/12% Nylon	Twill	FR	

TESTS CONDUCTED

Flame Resistance Test
Heat and Thermal Shrinkage Resistance Test
Thermal Protective Performance Test
Manikin Test

No additional testing was determined to be necessary.

File MH48828	Page T6-2 of 8	Issued:  2012-03-26
	New:  2015-02-06

FLAME RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.3	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Flame Resistance Test	8.3	03-LO-W0079	

2.0	RESULTS – FABRICS AND COLD WEATHER INSULATION MATERIALS

Article:	Outer Shell	
Description:	Model 8812FR, 7.1 OSY, 88% Cotton/12% Nylon Twill from Matchmaster Dyeing & Finishing	
Color:	White	
Unfinished Weight:	6.0	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Software Validation: 76083

File MH48828	Page T6-3 of 8	Issued:  2012-03-26
	New:  2015-02-06

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT'D)	NFPA 2112-2012, Section 8.3	

3.0	COMPLIANCE CRITERIA – FABRICS AND COLD WEATHER INSULATION MATERIALS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T6-4 of 8	Issued:  2012-03-26
	New:  2015-02-06

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.4	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat and Thermal Shrinkage Resistance Test	8.4	03-LO-W0035	

2.0	RESULTS - FABRICS

Article:	Outer Shell	
Description:	Model 8812FR, 7.1 OSY, 88% Cotton/12% Nylon Twill from Matchmaster Dyeing & Finishing	
Color:	White	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

Software Validation: 76083

File MH48828	Page T6-5 of 8	Issued:  2012-03-26
	New:  2015-02-06

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS (CONT'D)	NFPA 2112-2012, Section 8.4	

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T6-6 of 8	Issued:  2012-03-26
	New:  2015-02-06

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.2	

1.0	PROCEDURE

1.1	Test in accordance with:
TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat Transfer Performance (HTP) Test	8.2	03-LO-W0041	

2.0	RESULTS
Article:	Outer Shell	
Description:	Model 8812FR, 7.1 OSY, 88% Cotton/12% Nylon Twill from Matchmaster Dyeing & Finishing	
Color:	White	

CONDITIONING: SEE TABLE BELOW

Software Validation: 76083

3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than 25 J/cm2 
	(6.0 cal/cm2).
2. The average contact HTP rating shall not be less than 12.6 J/cm2 
(3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T6-7 of 8	Issued:  2012-03-26
	New:  2015-02-06

MANIKIN TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.5	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Manikin Test	8.5	03-LO-W0043	

2.0	RESULTS

Article:	Outer Shell	
Description:	Model 8812FR from Matchmaster Dyeing & Finishing	
Color:	White	
Test Report ID:	150204M, 150204N, 150204O	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	10.66	
2	9.02	
3	9.84	
Average	9.84	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T6-8 of 8	Issued:  2012-03-26
	New:  2015-02-06

Test Record No. 6 Summary

The results of this investigation, including construction review and testing, indicate that the products evaluated comply with the applicable requirements in NFPA 2112, Standard on Flame-Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition (2013-08-01) and, therefore, such products are judged eligible to bear UL's Mark as described on the Conclusion Page of this Report. Any information and documentation involving UL Mark services are provided on behalf of UL LLC (UL) or any authorized licensee of UL.

Test Record No. 6 By:	Reviewed By:	
		
Jessica Andrews	Andrew Kaiser	
Engineer	Senior Project Engineer	
Conformity Assessment Services	Conformity Assessment Services	

File MH48828	Page T7-1 of 11	Issued:  2012-03-26
	New:  2016-01-21

TEST RECORD NO. 7

The manufacturer submitted samples to perform testing per the requirements in NFPA 2112, Standard on Flame Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition (2013-08-01).  The results were in compliance with the requirements.

Results relate only to the items tested.

SAMPLES

Standard coveralls and yardage of the following fabrics:

Style Designation	Weight (oz/yd²)	Material Composition	Knit Type	Finish	
	Unfinished	Finished				
322XFR	7.7	8.5	86% Cotton/14% Polyester	Circular Knit	FR	
1950FM	6.0	6.6	93% Cotton/7% Spandex	Circular Knit	FR	

TESTS CONDUCTED

Flame Resistance Test
Heat and Thermal Shrinkage Resistance Test
Thermal Protective Performance Test
Manikin Test

No additional testing was determined to be necessary.

NOTE

A compacting process was added to Style 322XFR during the evaluation for Heat and Thermal Shrinkage Resistance testing.  The non-compacted version was evaluated for all other tests.  Since this is process does not impact the material composition and the test results far exceeded the minimum requirements, no further testing was deemed necessary.  

File MH48828	Page T7-2 of 11	Issued:  2012-03-26
	New:  2016-01-21

FLAME RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.3	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Flame Resistance Test	8.3	03-LO-W0079	

2.0	RESULTS – FABRICS AND COLD WEATHER INSULATION MATERIALS

Article:	Outer Shell Fabric	
Description:	Style 322XFR, 86% Cotton/14% Polyester, Circular Knit, Pyrosafe FR Finish, 8.5 OSY	
Color:	Navy	
Unfinished Weight:	7.7	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Software Validation: 76083

File MH48828	Page T7-3 of 11	Issued:  2012-03-26
	New:  2016-01-21

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT'D)	NFPA 2112-2012, Section 8.3	

3.0	COMPLIANCE CRITERIA – FABRICS AND COLD WEATHER INSULATION MATERIALS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T7-4 of 11	Issued:  2012-03-26
	New:  2016-01-21

FLAME RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.3	

2.0	RESULTS – FABRICS AND COLD WEATHER INSULATION MATERIALS

Article:	Outer Shell Fabric	
Description:	Style 1950FM, 93% Cotton/7% Spandex, Circular Knit, Pyrosafe FR Finish, 6.6 OSY	
Color:	Beige	
Unfinished Weight:	6.0	oz./yd²	

CONDITIONING: AS RECEIVED AND AFTER 100 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA – FABRICS AND COLD WEATHER INSULATION MATERIALS

3.1	1. Specimens shall not have an afterflame of more than 2 seconds average.
2. Specimens shall not have a char length of more than 100 mm (4 in.) average.
3. Specimens shall not melt or drip.

3.2	Results did comply with the requirements.

File MH48828	Page T7-5 of 11	Issued:  2012-03-26
	New:  2016-01-21

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS	NFPA 2112-2012, Section 8.4	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat and Thermal Shrinkage Resistance Test	8.4	03-LO-W0035	

2.0	RESULTS - FABRICS

Article:	Outer Shell Fabric	
Description:	Style 322XFR, 86% Cotton/14% Polyester, Circular Knit, Pyrosafe FR Finish with compacting process, 8.5 OSY	
Color:	Navy	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T7-6 of 11	Issued:  2012-03-26
	New:  2016-01-21

HEAT AND THERMAL SHRINKAGE RESISTANCE TEST – GARMENT MATERIALS (CONT’D)	NFPA 2112-2012, Section 8.4	

2.0	RESULTS - FABRICS

Article:	Outer Shell Fabric	
Description:	Style 1950FM, 93% Cotton/7% Spandex, Circular Knit, Pyrosafe FR Finish, 6.6 OSY	
Color:	Beige	

CONDITIONING: AS RECEIVED AND AFTER 3 LAUNDERINGS

Software Validation: 76083

3.0	COMPLIANCE CRITERIA - FABRICS

3.1	1. Specimens shall not shrink more than 10 percent in any direction.
2. Specimens shall not melt, drip, separate, or ignite.

3.2	Results did comply with the requirements.

File MH48828	Page T7-7 of 11	Issued:  2012-03-26
	New:  2016-01-21

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.2	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Heat Transfer Performance (HTP) Test	8.2	03-LO-W0041	

2.0	RESULTS

Article:	Outer Shell Fabric	
Description:	Style 322XFR, 86% Cotton/14% Polyester, Circular Knit, Pyrosafe FR Finish, 8.5 OSY	
Color:	Navy	

CONDITIONING: SEE TABLE BELOW

Software Validation: 76083

3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than 25 J/cm2 
	(6.0 cal/cm2).
2. The average contact HTP rating shall not be less than 12.6 J/cm2 
(3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T7-8 of 11	Issued:  2012-03-26
	New:  2016-01-21

HEAT TRANSFER PERFORMANCE (HTP) TEST – GARMENT FABRICS (CONT’D)	NFPA 2112-2012, Section 8.2	

2.0	RESULTS

Article:	Outer Shell Fabric	
Description:	Style 1950FM, 93% Cotton/7% Spandex, Circular Knit, Pyrosafe FR Finish, 6.6 OSY	
Color:	Beige	

CONDITIONING: SEE TABLE BELOW

Software Validation: 76083

3.0	COMPLIANCE CRITERIA

3.1	1. The average spaced HTP rating shall not be less than 25 J/cm2 
	(6.0 cal/cm2).
2. The average contact HTP rating shall not be less than 12.6 J/cm2 
(3.0 cal/cm2).
3. The individual HTP results shall be within 10% of the average HTP rating.

3.2	Results did comply with the requirements.

File MH48828	Page T7-9 of 11	Issued:  2012-03-26
	New:  2016-01-21

MANIKIN TEST – GARMENT FABRICS	NFPA 2112-2012, Section 8.5	

1.0	PROCEDURE

1.1	Test in accordance with:

TEST NAME	NFPA 2112-2012 SECTION	UL WORK INSTRUCTION	
Manikin Test	8.5	03-LO-W0043	

2.0	RESULTS

Article:	Outer Shell Fabric	
Description:	Style 322XFR, 86% Cotton/14% Polyester, Circular Knit, Pyrosafe FR Finish, 8.5 OSY	
Color:	Navy	
Test Report ID:	151020C, 151020D, 151020E	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	6.56	
2	6.56	
3	6.56	
Average	6.56	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T7-10 of 11	Issued:  2012-03-26
	New:  2016-01-21

MANIKIN TEST – GARMENT FABRICS (COND’T)	NFPA 2112-2012, Section 8.5	

2.0	RESULTS

Article:	Outer Shell Fabric	
Description:	Style 1950FM, 93% Cotton/7% Spandex, Circular Knit, Pyrosafe FR Finish, 6.6 OSY	
Color:	Beige	
Test Report ID:	151207D, 151207E, 151207F	

CONDITIONING: AFTER 1 LAUNDERING

Specimen	Predicted Percent Total Body Burn	
1	21.31	
2	67.21	
3	31.15	
Average	39.89	

3.0	COMPLIANCE CRITERIA

3.1	The average predicted body burn shall not exceed 50 percent.

3.2	Results did comply with the requirements.

File MH48828	Page T7-11 of 11	Issued:  2012-03-26
	New:  2016-01-21

Test Record No. 7 Summary

The results of this investigation, including construction review and testing, indicate that the products evaluated comply with the applicable requirements in NFPA 2112, Standard on Flame-Resistant Garments for Protection of Industrial Personnel Against Flash Fire, 2012 Edition (2013-08-01) and, therefore, such products are judged eligible to bear UL's Mark as described on the Conclusion Page of this Report. Any information and documentation involving UL Mark services are provided on behalf of UL LLC (UL) or any authorized licensee of UL.

Test Record No. 7 By:	Reviewed By:	
		
Andrew Kaiser	Nicholas B. Galloway	
Senior Project Engineer	Lead Engineering Associate	

File MH48828	Page C1	Issued:  2012-03-26

Conclusion

Samples of the components covered by this Report have been found to comply with the requirements covering the category and the components are found to comply with UL’s applicable requirements.  The description and test result in this Report are only applicable to the sample(s) investigated by UL and does not signify the product(s) described as being covered under UL’s Follow-Up Service Program.  When covered under UL’s Follow-Up Service Program, the manufacturer is authorized to use the Recognized Marking on such products which comply with UL’s Follow-Up Service Procedure and any other applicable requirements of UL LLC. The Recognized Component Mark of UL LLC on the product, or the Recognized Marking symbol on the product and the Recognized Component Mark on the smallest unit container in which the product is packaged, is the only method to identify products investigated by UL to published requirements and manufactured under UL’s Recognition and Follow-Up Service.

This Report is intended solely for the use of UL and the Applicant for establishment of UL certification coverage of the product under UL’s Follow-Up Service.  Any use of the Report other than to indicate that the sample(s) of the product covered by the Report has been found to comply with UL’s applicable requirements is not authorized and renders the Report null and void.  UL shall not incur any obligation or liability for any loss, expense, or punitive damages, arising out of or in connection with the use or reliance upon the contents of this Report to anyone other than the Applicant as provided in the agreement between UL and Applicant.  Any use or reference to UL’s name or certification mark(s) by anyone other than the Applicant in accordance with the agreement is prohibited without the express written approval of UL. Any information and documentation involving UL Mark services are provided on behalf of UL LLC (UL) or any authorized licensee of UL.

Report By:	Reviewed By:	
		
Andrew Kaiser	Amanda H. Newsom	
Project Engineer	Project Engineer	
Conformity Assessment Services	Conformity Assessment Services